## Slide 1: Mechanical Properties of Composite Materials
National Technical University of Athens
Athens 2022

## Slide 2: Micromechanics – Introduction
It is of great importance to be able to predict the properties of a composite, given the properties of the components and the geometric arrangement of the components in the composite.
A particularly simple case is the rule-of-mixtures, a rough tool that considers the composite properties as volume-weighted averages of the component properties. It is important to realize that the rule-of-mixtures works in only certain simple situations.
When more precise information is desired, it is better to use more sophisticated approaches based on the theory of elasticity.

## Slide 3: Micromechanics Prediction of Elastic Constants & Modulus
Unidirectional composite: (a) isostrain or action in parallel, (b) isostress or action in series
Variation of longitudinal modulus (E11) and transverse modulus (E22) with fiber volume fraction (Vf)

## Slide 4: Micromechanics Micromechanical Approaches
The states of stress and strain can each be described by six components.
An anisotropic body with no symmetry elements present requires 21 independent elastic constants to relate stress and strain  This is the most general case of elastic anisotropy.
In a generally anisotropic body, the two transverse strain components are not equal.
Any symmetry elements present will reduce the number of independent elastic constants
An elastically isotropic body, on the other hand, is the simplest case  it needs only two independent elastic constants
In such a body, when a tensile stress rz is applied in the z-direction, a tensile strain ez results in that direction. In addition to this tensile strain, there are two equal compressive strains (ex = ey) in thex- and y-directions.

## Slide 5: Micromechanics Micromechanical Approaches
A square array of fibers, for example, will have symmetry planes parallel to the fibers as well as perpendicular to them. Such a material is an orthotropic material  it has three mutually perpendicular planes of symmetry) and possesses nine independent elastic constants.
Hexagonal and random arrays of aligned fibers are transversely isotropic and have five independent elastic constants.
Various fiber arrays in a matrix: (a) square, (b) hexagonal, and (c) random

## Slide 6: Micromechanics Micromechanical Approaches
Elastic moduli of a transversely isotropic fibrous composite Adapted from Hashin and Rosen (1964)

## Slide 7: Micromechanics Micromechanical Approaches
Elastic constants of a transversely isotropic composite in terms of component constants (matrix isotropic, fiber anisotropic) Adapted from Chamis (1983)

## Slide 8: Micromechanics Micromechanical Approaches
A transversely isotropic fiber composite: plane transverse to fibers (2–3 plane) is isotropic

## Slide 9: Micromechanics Solving the elasticity problem
The elasticity problem is then solved by a series development, a complex variable technique, or a numerical solution.
The approach of Eshelby (1957, 1959) considers an infinite matrix containing an ellipsoidal inclusion. Modifications of the Eshelby method have been made by Mori and Tanaka (1973).
The variational or bounding methods focus on the upper and lower bounds on elastic constants.
  When the upper and lower bounds coincide, the property is determined exactly.
  Frequently, the upper and lower bounds are well separated.
  When these bounds are close enough, we can safely use them as indicators of thematerial behavior.

## Slide 10: Micromechanics Example
Consider a unidirectionally reinforced glass fiber/epoxy composite. The fibers are continuous and 60% by volume. The tensile strength of glass fibers is 1 GPa, and the Young’s modulus is 70 GPa. The tensile strength of the epoxy matrix is 60 MPa, and its Young’s modulus is 3 GPa. Compute the Young’s modulus and the tensile strength of the composite in the longitudinal direction.
Solution
Young’s modulus of the composite in the longitudinal direction is given by: Ecl = 70 Χ 0.6 + 3 Χ 0.4 = 42 + 1.2 = 43.2 Gpa
To calculate the tensile strength of the composite in the longitudinal direction, we need to determine which component, fiber or matrix, has the lower failure strain.
The failure strain of the fiber is: ε = σf / Ef = 1/70 = 0.014
while that of the matrix is: εm = (60 Χ 10-3)/3 = 0.020

## Slide 11: Micromechanics Example (continue)
Thus, εf < εm, i.e., fibers fail first. At that strain, assuming a linear stress–strain curve for the epoxy matrix, the matrix strength is:
σ’m = Em εf = 3 Χ 0.014 = 0.042 Gpa
Then, we get the composite tensile strength as:
σc = 0.6 Χ 1 + 0. 4 Χ 0.042 = 0.6 + 0.0168 = 617MPa

## Slide 12: Micromechanics Transverse Stresses
A single fiber surrounded by its matrix shell
Three-dimensional stress distribution (schematic) in the unit composite shown in next Figure. In this case, the transverse stresses (σr and σθ) result from the differences in the Poisson’s ratios of the fiber and matrix

## Slide 13: Micromechanics Thermal Properties
Thermal energy is responsible for the atomic or molecular vibration about a mean position in any material. As the temperature of a material is increased, the amplitude of thermal energy-induced vibrations is increased and the interatomic or intermolecular spacing increases, i.e., an expansion of the body occurs
Most materials show such an expansion with increasing temperature. In general, the thermal expansion of a material is greater in the liquid state than in the crystalline state, with the transition occurring at the melting point.
In the case of a glassy material, such a transition occurs at the glass transition temperature, although it is not as well defined as the one at the melting point.
Over a certain range of temperature, one can relate the temperature interval and thermal strain by a coefficient, called the coefficient of thermal expansion.

## Slide 14: Micromechanics - Thermal Properties
Longitudinal and transverse linear thermal expansion coefficients versus fiber volume fraction for a composite of alumina fiber in an aluminum matrix
Thermal properties of a transversely isotropic composite (matrix isotropic, fiber anisotropic)
Adapted from Chamis (1983)

## Slide 15: Micromechanics - Example
A unidirectional glass fiber reinforced epoxy has 50 vol% of fiber. Estimate its thermal conductivity parallel to the fibers. Given kglass = 0.9 W/mK, kepoxy = 0.15 W/mK.
Solution
Glass fiber is isotropic, i.e., kf1 = kf2 = kf. The longitudinal thermal conductivity is given by:
kct = Vmkm + Vfkf
= 0.5 Χ 0.15 + 0.5 Χ 0.9
= 0.075 + 0.45 = 0.525 W/mK

## Slide 16: Micromechanics - Electrical Conductivity
Electrical conductivity (or its inverse electrical resistivity) is another important physical property.
In terms of electrical conductivity, composites represent a mixed bag.
PMCs and CMCs are generally poor electrical conductors.
The electrical conductivity of polymers can be increased by the addition of carbon fibers, carbon black, and graphite particles.
Physical properties such as thermal and electrical conductivity of composites depend on the properties of the matrix and reinforcement, their volume fractions, characteristics of the interface region, shape of the reinforcement, and the connectivity of the phases.
The conductivity (thermal or electrical) of a composite will depend on conductivity characteristics of the matrix, reinforcement, volume fraction and aspect ratio of the reinforcement, and, of course, the interfacial characteristics. In particular, interfacial resistance will vary with the form and size of reinforcement.

## Slide 17: Micromechanics Hygral and Thermal Stresses
Hygroscopy, the ability of a substance to absorb water, can be a problem with polymeric resins and natural fibers because it can lead to swelling. Swelling can lead to stresses if, as is likely in a composite, the material is not allowed to expand freely because of the presence of a second component.
Such stresses resulting from moisture absorption or hygroscopy are called hygral stresses.
Thermal stresses will result in a material when the material is not allowed to expand or contract freely because of a constraint.
When both hygral and thermal stresses are present, we call them hygrothermal stresses.
Mathematically, these two types of internal stresses are quite similar, and we can treat them together.

## Slide 18: Micromechanics – Hygral and Thermal Stresses
(a) Strain-free reference state; (b) thermal strain (eT); (c) hygral (eH) and thermal (eT) strains; and ( d) final state: hygral (eH), thermal (eT), and mechanical strain

## Slide 19: Micromechanics Thermal Stresses in Composites
During curing or solidification of the matrix around reinforcement fibers or particles, a large magnitude of shrinkage stresses can result.
The thermal stresses generated depend on the reinforcement volume fraction, reinforcement geometry, thermal mismatch (Δα), and the modulus ratio, Er/Em where E is the Young’s modulus and the subscripts r and m refer to the reinforcement and matrix, respectively.
Generally, αm > αf, that is, on cooling from T0 to T (T0 > T), the matrix would tend to contract more than the fibers, causing the fibers to experience axial compression.
In extreme cases, fiber buckling can also lead to the generation of interfacial shear stresses. This problem of thermal stresses in composite materials is a most serious and important problem.
It is worth repeating that thermal stresses are internal stresses that arise whenever there is a constraint on the free dimensional change of a body

## Slide 20: Micromechanics – Thermal Stresses in Composites
Three-dimensional thermal stress state in a tungsten fiber/copper matrix composite for two different volume fractions. Note the change in rz level with Vf. (From Chawla and Metzger 1972)
Variation of dislocation density (≃ pit density) with distance from the interface. The higher dislocation density in the plateau region with high Vf is due to a higher rz with higher Vf (next figure).
(From Chawla and Metzger 1972,

## Slide 21: Micromechanics Thermal Stresses in Composites
(a) Dislocations generated at SiC whiskers in an aluminum matrix in an in situ thermal cycling experiment done in a high-voltage electron microscope. (From Vogelsang et al. 1986); (b) Cracking in the CaTiO3 layer in a CaTiO3/Al2O3 composite due to thermal stresses generated during cooldown from the processing temperature.(From Gladysz and Chawla2001)

## Slide 22: Micromechanics Thermal Stresses in Composites
The particulate form of reinforcement can result in a considerably reduced degree of anisotropy.
However, so long as a thermal mismatch exists between the particle and the matrix, thermal stresses will be present in such composites as well.
A particle reinforced composite

## Slide 23: Micromechanics Thermal Stresses in Composites
Spherical coordinate system.
Stress distribution in a particulate composite for cooldown from the processing temperature

## Slide 24: Micromechanics Mechanics of Load Transfer from Matrix to Fiber
The topic of load transfer from the matrix to the fiber has been treated by a number of researchers.
The matrix holds the fibers together and transmits the applied load to the fibers, the real load-bearing component in most cases.
Transfer of the applied load to the fiber thus occurs by means of these shear strains in the matrix.
A high modulus fiber embedded in a low modulus matrix: (a) before deformation,
(b) after deformation

## Slide 25: Micromechanics Fiber Elastic–Matrix Elastic
Load transfer in a fiber/matrix composite: Variation of tensile stress (rf) in the fiberand interfacial shear stress (τ) with distance along the interface

## Slide 26: Micromechanics Fiber Elastic–Matrix Elastic
Τhe finite difference method to show the high shear strains in the matrix near the fiber extremities.
Micro-Raman spectroscopy has been used to study the deformation behavior of organic and inorganic fiber reinforced composites.
Characteristic Raman spectra can be obtained from these fibers in the undeformed and the deformed states. Under tension, the peaks of the Raman bands shift to lower frequencies. The magnitude of frequency shift is a function of the material, Raman band under consideration, and the Young’s modulus of the material.
The shift in Raman bands results from changes in force constants due to changes in molecular or atomic bond lengths and bondangles.
Micro-Raman spectroscopy is a very powerful technique that allows us to obtain point-to-point variation in strain along the fiber length embedded in a transparent matrix.

## Slide 27: Micromechanics - Fiber Elastic–Matrix Elastic
Micro-Raman spectra of Kevlar aramid 149 when the Kevlar/epoxy composite is loaded axially. (a),(b) strain buildup in the fiber from the two ends. (c), (d) fiber fracture leads to a drop in strain at those sites. (After Young, 1994).

## Slide 28: Micromechanics - Fiber Elastic–Matrix Plastic
It should be clear from the preceding discussion that in order to load high strength fibers in a ductile matrix to their maximum strength, the matrix shear strength must be large.
A metallic matrix will flow plastically in response to the high shear stresses developed.
Of course, if the shear strength fiber/matrix interface is less than the shear yield strength of the matrix, then the interface will fail first.
Schematic of variation of tensile stress in a fiber (σf) and interface shear stress (τ) with different fiber aspect ratios (l/d)

## Slide 29: Micromechanics Load Transfer in Particulate Composites
The shear lag model described in the previous section is suitable for explaining the load transfer from the matrix to a high aspect ratio reinforcement via shear along the interface parallel to the loading direction
A modified shear lag model predicts a linear but modest increase in the strength of the composite with particle volume fraction. However, no account is taken of the particle size or other microstructural parameters.
Models involving the modified shear lag model, Eshelby’s equivalent inclusion approach, and Weibull statistics have been proposed
Micromechanics Fiber Elastic–Matrix Plastic
In MMCs, assuming that the plastically deforming matrix does not work harden, the shear stress at the fiber surface, τ(rf), will have an upper limit of τy, the matrix shear yield strength.
In PMCs and CMCs, frictional slip at the interface is more likely than plastic flow of the matrix

## Slide 30: Macromechanics - Introduction
Laminated fibrous composites are made by bonding together two or more laminae.
These composites, frequently referred to as laminates, are different from sheet laminates made by bonding flat sheets of isotropic materials.
In a laminated fibrous composite, the individual unidirectional laminae or plies are oriented in such a manner that the resulting structural component has the desired mechanical and/or physical characteristics in different directions.
Thus, one exploits the inherent anisotropy of fibrous composites to design a composite material with appropriate properties

## Slide 31: Macromechanics - Introduction
Macromechanical analysis of laminate composites. A unidirectional ply is treated as a homogeneous, orthotropic material. Many such plies are stacked in an appropriate order (following laminated plate or shell theory) to make the composite

## Slide 32: Macromechanical Analysis (step 1)
While micromechanics is very useful in analyzing the composite behavior, we use the information obtained from a micromechanical analysis of a thin unidirectional lamina (or in the case of a lack of such analytical information, we must determine experimentally the properties of the lamina) as input for a macromechanical analysis of a laminated composite
An off-axis unidirectional lamina
A thin lamina with natural (or material) axes coinciding with the geometric axes

## Slide 33: Macromechanical Analysis (step 2)
Once we have determined, analytically or otherwise, the characteristics of a fibrous lamina, we ignore its detailed microstructural nature and simply treat it as a homogeneous, orthotropic sheet.
A laminated fibrous composite is made by stacking a number of such orthotropic fiber reinforced plies or sheets at specific orientations to get composite laminate with the desired characteristics.
We then use the well established theory of laminated plates or shells to analyze macromechanically such laminated composites.

## Slide 34: Macromechanical Variation of Lamina Properties with Orientation
Variation of elastic constants with fiber orientation angle for a 50 v/o carbon/epoxy composite: (a) longitudinal and transverse Young’s moduli (Ex and Ey), (b) shear modulus (Gxy), and (c) Poisson’s ratio (vx and vy)

## Slide 35: Macromechanical Analysis of Laminated Composites
We assume that the laminate thickness is small compared to its lateral dimensions.  Therefore, stresses acting on the interlaminar planes in the interior of the laminate, that is, away from the free edges, are negligibly small (we shall see later that the situation is different at the free edges).
We also assume that there exists a perfect bond between any two laminae.  That being so, the laminae cannot slide over each other, and we have continuous displacements across the bond
We make yet another important assumption, namely, a line originally straight and perpendicular to the laminate midplane remains so after deformation. Actually, this follows from the perfect bond assumption, which does not allow sliding between the laminae.
Finally, we have the so called Kirchhoff assumption, which states that inplane displacements are linear functions of the thickness, and therefore the interlaminar shear strains, εxz and εyz, are negligible,

## Slide 36: Macromechanical Analysis of Laminated Composites
A laminate composite with the stacking sequence given by [01/902/–453/453]s

## Slide 37: Macromechanical Analysis of Laminated Composites
Strains vary through the thickness of laminated composite linearly with thickness; the stresses do not.
This is easy to visualize if we recall that stiffness of each ply will be different; being a function of the fiber orientation.
These resultants of stresses and moments acting on a laminate cross section, defined as follows, provide us with a statically equivalent system of forces and moments acting at the midplane of the laminated composite
(a) A laminated composite made up of n stacked plies. (b) Variation of strain and stress through the thickness in a 4-ply laminated composite

## Slide 38: Macromechanical Analysis of Laminated Composites
Force (N) and moment (M) resultants in a laminated composite

## Slide 39: Macromechanical Analysis of Laminated Composites
If for each +θ ply, we have another identical ply of the same thickness at −θ, then we shall have what is called a specially orthotropic laminate with respect to inplane stresses and strains; that is, A16 = A26 = 0.
The relative position of such plies in the stacking sequence does not matter,
Τhe Bij are zero if we have for each ply above the midplane a ply identical in properties and orientation and at an equal distance below the midplane. Such a laminate is called a symmetric laminate and will have Bij identically zero.
Some special laminates

## Slide 40: Macromechanical Analysis of Laminated Composites
The important results of this section can be summarized as follows:

## Slide 41: Macromechanical Interlaminar Stresses and Edge Effects
We may regard the interlaminar stresses as a boundary layer phenomenon restricted to the free edge and extending inward a distance equal to the laminate thickness.
A four-ply laminate (±θ, thickness 4h0) under a uniform axial strain

## Slide 42: Macromechanical Interlaminar Stresses and Edge Effects
Using the classical lamination theory to describe the laminate composite behavior is rigorously correct for an infinite laminate composite.
It turns out that the assumption of a generalized plane stress state is quite valid in the interior of the laminate, that is, away from the free edges.
At and near the free edges (extending a distance approximately equal to the laminate thickness) there exists, in fact, a three-dimensional state of stress.
Under certain circumstances, there can be rather large interlaminar stresses present at the free edges, which can lead to delamination of plies or matrix cracking at the free edges and thereby cause failure.

## Slide 43: Macromechanical Interlaminar Stresses and Edge Effects
Stress distribution at the interface z = h0 as a function of y/b, where 2b is the laminate width. Note the high value of σxy at the free edge; σxy falls approximately to zero at y/b = 0.5

## Slide 44: Macromechanical Interlaminar Stresses and Edge Effects
We can summarize the edge effects in laminated composites as follows:
The classical lamination theory of plates inplane stress is valid in the laminate interior, provided the laminate is sufficiently wide (i.e., b/4h0 >>2).
Interlaminar stresses are confined to narrow regions of dimensions comparable to the laminate thickness and adjoining the free edges (i.e., y = ± b).
The ply stacking sequence in a laminate affects the magnitude as well as the sign of the interlaminar stresses, which in turn affects the mechanical performance of the laminate. Specifically, a tensile interlaminar stress at the free edge is likely to cause delaminations.

## Slide 45: Macromechanical Interlaminar Stresses and Edge Effects
Surface displacements of a symmetric angle-ply laminate subjected to axial tension. Experimental data points were determined by the Moiré technique

## Slide 46: Monotonic Strength and Fracture Tensile Strength of Unidirectional Fiber Composites
The term monotonic behavior means behavior under an applied stress that increases in one direction, i.e., not a cyclic loading condition.
The important question here is: What is the value of the matrix stress, σm?  Ideally, it should be the in situ value of the stress on the matrix at a given strain.
The main reason that the rule-of-mixtures does not always work for predicting the strength of a composite, while it works reasonably well for Young’s modulus in the longitudinal direction, is that the elastic modulus is a relatively microstructure-insensitive property while strength is a highly microstructure-sensitive property.
Because the strength is an extremely structure-sensitive property, synergism can occur in regard to composite strength.
Matrix or fiber structure may be altered during fabrication.
Composite materials consist of two components whose thermomechanical properties are generally quite different and thus may have residual stresses and/or undergo structural alterations owing to these internal stresses.
Another source of microstructural modification of a component is a phase transformation induced by the fabrication process.
The matrix stress state may also be influenced by rheological interaction between the components during straining.
In view of this, the rule-of-mixtures should be regarded, in the best of circumstances, as an order of magnitude indicator of the strength of a composite.

## Slide 47: Monotonic Strength and Fracture Compressive Strength of Unidirectional Fiber Composites
Fiber reinforced composites under compressive loading can be regarded, as a first approximation, as elastic columns under compression  the main failure modes in the failure of a composite are the ones that occur in the buckling of columns.
Buckling occurs when a slender column under axial compression becomes unstable against lateral movement of the central portion.
Fiber reinforced composites fail, in compression, by periodic buckling of the fibers, with the buckling wavelength being proportional to the fiber diameter.
If we were to put the same fiber in two different matrices (i.e., with different matrix moduli), we should be able to distinguish between these two compressive failure modes.
An out-of-phase buckling mode predominated at low fiber volume fractions.
At high fiber volume fractions, fibers exerted more influence on each other and a coupled or in-phase buckling mode prevailed

## Slide 48: Monotonic Strength and Fracture Compressive Strength of Unidirectional Fiber Composites
Fiber reinforced composites under compressive loading can be regarded, as:
(a) Unbuckled fiber reinforced composite,
(b) in-phase buckling of fibers under compression, and
(c) out-of-phase buckling of fibers under compression

## Slide 49: Monotonic Strength and Fracture Compressive Strength of Unidirectional Fiber Composites
Compressive strength of MMCs is generally higher than that of PMCs
It has been observed a compressive strength ≥ 4 GPa for aluminum alloy matrix containing high fiber volume fraction (55–65%) Nextel 610 alumina fibers. Fiber microbuckling was the observed failure mode.
Kink bands initiate from a damage zone comprising crushed and broken fibers. When the damage zone reached a critical size, the unsupported column of matrix caused a local matrix shear instability (or microbuckling).  This local instability propagated as a kink band.  The damage zone angle was found to depend on the interface properties, and it affected the strain to form kink bands. In the case of a laminated composite, poor interlaminar bonding can result in easy buckling of fibers.
Heat and moisture as well as the ply stacking sequence can also affect the compressive strength.

## Slide 50: Monotonic Strength and Fracture Fracture Modes in Tension
A large variety of deformation modes can lead to failure of the composite
The operative failure mode depends, among other things, on loading conditions and the microstructure of a particular composite system.
By microstructure, we mean fiber diameter, fiber volume fraction, fiber distribution, and damage resulting from thermal stresses that may develop during fabrication and/or in service.
In view of the fact that many factors can and do contribute to the fracture process in composites, it is not surprising that a multiplicity of failure modes is observed in a given composite system.

## Slide 51: Monotonic Strength and Fracture Fracture Modes in Tension - Single and Multiple Fracture
In general, the fiber and matrix will have different values of strain at fracture.
When the component that has the smaller breaking strain fractures, for example, a brittle fiber or a brittle ceramic matrix, the load carried by this component is thrown onto the other one.
If the component with a higher strain of fracture can bear this additional load, the composite will show multiple fractures of the brittle component.
A manifestation of this phenomenon is fiber bridging of the ceramic matrix.
Eventually, a particular transverse section of the composite becomes so weak that the composite is unable to carry the load any further and it fails.

## Slide 52: Monotonic Strength and Fracture Fracture Modes in Tension - Single and Multiple Fracture
Strength of the composite versus fiber volume fraction showing the conditions for single and multiple fiber fracture.

## Slide 53: Monotonic Strength and Fracture Fracture Modes in Tension – Debonding, Fiber Pullout, and Delamination Fracture
Debonding of the fiber/matrix interface, fiber pullout, and delamination fracture are some of the features that are commonly observed in fiber reinforced composites;  these modes of fracture are not observed in conventional, monolithic materials.
The final fracture of the composite will generally involve some fiber pullout.
If this fiber is pulled out, the bonding between the matrix and the fiber will produce a shear stress τ parallel to the fiber surface.
For maximum fiber strengthening, we would like the fiber to break rather than be pulled out of the matrix
From a toughness point of view, however, fiber pullout may be more desirable.

## Slide 54: Monotonic Strength and Fracture Fracture Modes in Tension – Debonding, Fiber Pullout, and Delamination Fracture
Real fibers do not have uniform properties but rather show a statistical distribution.  Weak points are distributed along the fiber length.
It is more than likely that a fiber would break away from the main fracture plane.
Interfacial debonding occurs around the fiber breakpoint.
The broken fiber parts are pulled out from their cylindrical holes in the matrix during further straining.
A fiber of length l, embedded in a matrix, being pulled out

## Slide 55: Monotonic Strength and Fracture Fracture Modes in Tension - Debonding, Fiber Pullout, and Delamination Fracture
(a) Schematic of fiber pullout in a continuous fiber composite.
(b) Fiber pullout in a B/Al system. Fiber diameter is 140 μm.
(c) Schematic of an isolated fiber pullout through a distance x against an interfacial shear stress,τi

## Slide 56: Monotonic Strength and Fracture Fracture Modes in Tension – Debonding, Fiber Pullout, and Delamination Fracture
In general, fiber pullout provides a more significant contribution to composite fracture toughness than fiber/matrix debonding.
Debonding must precede pullout.
Work is done in the debonding process as well as in fiber pullout against frictional resistance at the interface.
As the fiber length increases, an increasing fiber length will be pulled out.
The fiber length l should be large but close to lc for maximizing the fiber pullout work and to prevent the composite from separating into two halves.
It should be recognized at the same time that for l < lc, the fiber will not get loaded to its maximum possible strength level and thus full fiber strengthening potential will not be realized

## Slide 57: Monotonic Strength and Fracture Fracture Modes in Tension - Debonding, Fiber Pullout, and Delamination Fracture
Variation of work done in fiber pullout with fiber length

## Slide 58: Monotonic Strength and Fracture Fracture Modes in Tension – Debonding, Fiber Pullout, and Delamination Fracture
One measure of fracture toughness can loosely be defined as resistance to crack propagation.
Consider a fiber reinforced composite containing a crack transverse to the fibers. In such a situation, we can increase the crack propagation resistance by one of the following means, each of which involves additional work:
  Plastic deformation of the matrix (applicable in a metal matrix).
  2. Presence of weak interfaces, fiber/matrix separation, and deflection of the crack.
  3. Fiber pullout.
A delamination type fracture of Kevlar/epoxy composite. Note the characteristic fibrillation in the fiber

## Slide 59: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
Most high performance fibers are brittle.  Thus, their strength must be characterized by a statistical distribution function.
There are many statistical distribution functions for the strength of a material.
Work is done in the debonding process as well as in fiber pullout against frictional resistance at the interface.
For brittle materials, a distribution function called the Weibull statistical distribution function (named after the Swedish engineer who first proposed it) has been found to characterize the strength of fairly well
For high strength fibers also, the Weibull treatment of strength has been found to be quite adequate

## Slide 60: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
(a) Strength distribution for a brittle material. (b) Strength distribution for material with insignificant variability of strength

## Slide 61: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
Normalized mean fiber strength versus fiber length L
For b = 10, which corresponds to a μ≈ 12%, an order of magnitude increase in fiber length produces a 20% fall in average strength. For b = 4, the corresponding fall in strength is about 50%.

## Slide 62: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
If we use Weibull statistics to characterize ceramic fibers, we can answer the following important question: For making tough, strong fiber reinforced ceramic matrix composites, would we want fibers with small or large Weibull modulus?
The lower the Weibull modulus of ceramic fibers (i.e., the less uniformity in their properties), the more graceful failure of the CMC.
It is understandable if we recall that a low Weibull modulus fiber will fracture in the composite at different strain values and thus spread the damage, which would lead to final non-catastrophic failure of the CMC.

## Slide 63: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
Fiber bundle strength versus strain in a CMC for different Weibull modulus values
Normalized fiber bundle strength versus variance μ of the fiber population

## Slide 64: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
In view of the statistical distribution of fiber strength, it is natural to extend these ideas to composite strength.  We present here the treatment called cumulative weakening model of failure.
When we load a fiber reinforced composite, fibers (assuming they are more brittle than the matrix) fracture at various points before a complete failure of the composite occurs.
There occurs an accumulation of fiber fractures with increasing load.
At a certain point, one transverse section will be weakened as a result of the statistical accumulation of fiber fractures, hence the name cumulative weakening model of failure.
Because the fibers have nonuniform strength, it is expected that some fibers will break at very low stress levels.

## Slide 65: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
Perturbation of stress state caused by a fiber break
Fracture models: (a) fiber fracture leading to interfacial delamination, (b) first fiber fracture leading to a complete fracture of the composite, and (c) cumulative damage by multiple fiber fracture leading to a statistical distribution of fiber breaks

## Slide 66: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
At the point of fiber fracture, the tensile stress in the fiber drops to zero.
From this point onward, the tensile stress in the fiber increases along the fiber length along the two fiber segments as per the load transfer mechanism by interfacial shear.
As a result, either the matrix would yield in shear or an interfacial failure would occur.
Additionally, this local drop in stress caused by a fiber break will throw the load onto adjoining fibers, causing stress concentrations there.
Upon continued straining, progressive fiber fractures cause a cumulative weakening and a redistribution of the load in the composite.

## Slide 67: Monotonic Strength and Fracture Effect of Variability of Fiber Strength
Normalized composite strength σ*C / σL, versus variance μ

## Slide 68: Monotonic Strength and Fracture Strength of an Orthotropic Lamina
Fiber reinforced composites have anisotropic properties. This results from the fact that the fibers are aligned in the matrix. Additionally, the fibers are, generally, a lot stiffer and stronger than the matrix. Therefore, not unexpectedly, fiber reinforced composites also show anisotropy in strength properties.
Quite frequently, the strength in the longitudinal direction is as much as an order of magnitude greater than that in the transverse direction.
It is of great importance for design purposes to be able to predict the strength of a composite under the loading conditions prevailing in service.
The use of a failure criterion gives us information about the failure strength under combined stresses.
  Maximum Stress Criterion
  Maximum Strain Criterion
  Maximum Work (or the Tsai–Hill) Criterion
  Quadratic Interaction Criterion

## Slide 69: Monotonic Strength and Fracture Strength of an Orthotropic Lamina
Maximum Stress Criterion: Failure of fiber reinforced lamina will occur when any one of the stress components is equal to or greater than its corresponding allowable or intrinsic strength.
Variation of strength with fiber orientation for boron/epoxy. Quadratic interaction criterion (solid curve) shows better agreement with experimental data than the maximum stress criterion (dashed curve)

## Slide 70: Monotonic Strength and Fracture Strength of an Orthotropic Lamina
Maximum Strain Criterion: This criterion is analogous to the maximum stress criterion. Failure occurs when any one of the strain components is equal to or greater than its corresponding allowable strain.
Maximum Work (or the Tsai–Hill) Criterion: According to the Tsai–Hill criterion, failure of an orthotropic lamina will occur under a general two-dimensional stress state when the following expression holds:
  where X1, X2, and S are the longitudinal tensile failure strength, the transverse tensile failure strength, and the in plane shear failure strength, respectively. If compressive stresses are involved, then the corresponding compressive failure strengths should be used. This criterion does take into account the interaction between the failure modes. However, it does not make any direct distinction between tensile and compressive stresses.

## Slide 71: Monotonic Strength and Fracture Strength of an Orthotropic Lamina
Quadratic Interaction Criterion: As the name indicates, this criterion takes into account the stress interactions. According to this theory, the failure surface in stress space can be described by a function of the form:
f(σ) = Fiσi + Fijσiσj = 1 i, j = 1, 2, 6
  where Fi and Fij are the strength parameters. For the case of plane stress, i,j = 1,2,6

## Slide 72: Monotonic Strength and Fracture Strength of an Orthotropic Lamina
Comparison of failure theories

## Slide 73: Monotonic Strength and Fracture Strength of an Orthotropic Lamina
Failure envelopes due to different failure criteria. The shaded past indicates the conservative failure region

## Slide 74: Fatigue and Creep Introduction
Fatigue is the phenomenon of mechanical property degradation leading to failure of a material or a component under cyclic loading. The operative word in this definition is cyclic. This definition thus excludes the so called phenomenon of static fatigue, which is sometimes used to describe stress corrosion cracking in glasses and ceramics in the presence of moisture.
Creep refers to time-dependent deformation in a material, which becomes important at relatively high temperatures (T > 0.4Tm, where Tm is the melting point in kelvin).
There are many applications of composites where cyclic fatigue and high temperature (i.e., creep) conditions prevail.

## Slide 75: Fatigue and Creep Fatigue
The application of conventional approaches to fatigue of composites, for example, the stress versus cycles (S–N) curves or the application of linear elastic fracture mechanics (LEFM), is not straightforward. The main reasons for this are the inherent heterogeneity and anisotropic nature of the composites.
The fracture behavior of composites is characterized by a multiplicity of damage modes:
  matrix crazing (in a polymeric matrix),
  matrix cracking (in a brittle matrix),
  matrix plasticity (in a ductile matrix),
  fiber fracture,
  interfacial debonding and
  delamination,
  void growth,
  multidirectional cracking,
these modes appear rather early in the fatigue life of composites.

## Slide 76: Monotonic Strength and Fracture Fatigue
Diffuse damage zone in a fiber reinforced composite (anisotropic): (a) fiber break and local debonding; (b) matrix cracking; (c) deflection of the principal crack along a weak fiber/matrix interface

## Slide 77: Monotonic Strength and Fracture Fatigue
Some useful parameters for fatigue

## Slide 78: Monotonic Strength and Fracture Fatigue
S–N curves are commonly used with monolithic materials, especially metals and, to some extent, with polymers. It involves determination of the so-called S–N curves
S (or σa) is the stress amplitude and N is the number of cycles to failure. In general, for ferrous metals, one obtains a fatigue limit or endurance limit.
The variety of operating mechanisms and the inadequacy of the S–N curve approach have been documented by many researchers
S–N curves of unreinforced polysulfone (PSF) and composites with a PSF matrix and different amounts of short fibers (glass and carbon). The S–N curves move up with increasing fiber volume fraction.
Hysteretic temperature rise under fatigue for glass fiber/polypropylene composites. At a given stress amplitude, temperature rises more quickly at higher frequency and leads to premature failure of the composite

## Slide 79: Monotonic Strength and Fracture Fatigue
In general, the fibers provide a crack-impeding effect but the nature of the fiber (morphology, rigidity, and fracture strain), the fiber/interface, and/or any reaction zone phases that might form at the interface can have great influence.
For the crack arrest geometry, if the interface is weak, then the crack on reaching the interface bifurcates and changes its direction and thus the failure of the composite is delayed.
The improved fatigue crack propagation resistance in crack divider geometry has been attributed either to interfacial separation, which relieves the triaxial state of stress, or to an interfacial holding back of crack in the faster crack-propagating component by the slower crack-propagating component.
In unidirectional composites the fatigue resistance will be maximum along the fiber direction and the greatest efficiency will be achieved if the fibers have uniform properties, as much as possible defect-free, and much stronger than the matrix.
due to the highly anisotropic nature of the fiber reinforced composites in general, the fatigue strength of any off-axis fibrous composite will be expected to decrease with increasing angle between the fiber axis and the stress axis.

## Slide 80: Monotonic Strength and Fracture Fatigue
(a) S–N curves for MMCs in tension–tension for unidirectionally reinforced boron fiber (40% v/o)/A16061, alumina fiber (50% v/o)/Al, and alumina fiber (50% v/o)/Mg composites. (b) S–N curves for silicon carbide particle reinforced aluminum matrix composites

## Slide 81: Monotonic Strength and Fracture Fatigue
Particle or short fibers can provide easy crack initiation sites. The detailed behavior can vary depending on the volume fraction of the reinforcement, shape, size, and most importantly on the reinforcement/matrix bond strength.
Some possible reinforcement and crack tip interactions

## Slide 82: Monotonic Strength and Fracture Fatigue
Crack growth rate, da/dN, is related to the cyclic stress intensity factor range, ΔK, according to the power law relationship formulated by Paris and Erdoga:
da /dN = A(ΔK)m
  where A and m are constants that depend on the material and test conditions. The applied cyclic stress intensity range is given by:
ΔΚ=ΥΔσ
where Y is a geometric factor, Δσ is the cyclic stress range, and a is the crack length.
The major problem in this kind of test is to make sure that there is one and only one dominant crack that is propagating.

## Slide 83: Monotonic Strength and Fracture Fatigue
In a conventional, homogeneous material, the term damage simply represents the crack length, and not surprisingly it increases monotonically with cycling.
In the case of a laminate, we do not have a simple and unambiguous manifestation of damage, such as a crack length. Instead, damage is diffused and involves a variety of cracks, so damage, in principle, would mean the crack density.
This distinctive behavior is very important.
(a) Comparison of damage accumulation as a function of fatigue cycles in a laminated composite (made by appropriately stacking differently oriented plies) and a monolithic, homogeneous material under constant stress amplitude fatigue. (b) Fracture surface of B(W)/A1 6061 composite made by diffusion bonding. Note the different modes of damage: ductile fracture in aluminum, brittle fracture in boron, fiber pullout (see the missing fiber in top-left-hand corner), and sheet delamination

## Slide 84: Monotonic Strength and Fracture Fatigue
The fiber reinforced laminates can sustain a variety of subcritical damage (crazing and cracking of matrix, fiber/matrix decohesion, fiber fracture and pullout, ply cracking, delamination, and so on).
In the first stage, homogeneous, noninteractive cracks appear in individual plies. In the second stage, the damage gets localized in zones of increasing crack interaction. The transition from stage one to stage two occurs at what has been called the characteristic damage state (CDS), which consists of a well-defined crack pattern characterizing saturation of the noninteractive cracking.
Schematic of changes in crack density, delamination, and modulus in a composite
laminate under fatigue

## Slide 85: Monotonic Strength and Fracture Fatigue
It was mentioned earlier that the complexities in composites lead to the presence of many modes of damage, such as matrix cracking, fiber fracture, delamination, debonding, void growth, and multidirectional cracking.
These modes appear rather early in the fatigue life of composites, i.e., these subcritical damage accumulation mechanisms come into play rather early in the fatigue life—well before the fatigue limit, as determined in an S–N test, and a highly diffused damage zone is formed.
The scatter in fatigue data of composites are much greater than that in fatigue of monolithic, homogeneous materials because of the existence of a variety of damage mechanisms in composites, to wit, random distribution of matrix microcracks, fiber/matrix interface debonding, and fiber breaks, etc. With continued cycling, an accumulation of damage occurs. This accumulated damage results in a reduction of the overall stiffness of the composite laminate. Measurement of stiffness loss as a function of cycling has been shown to be quite a useful technique for assessing the fatigue damage in composites. Information useful to designers can be obtained from such curves

## Slide 86: Monotonic Strength and Fracture Fatigue
Typical modulus loss curve for unidirectional silicon carbide/aluminum composites. EN is the modulus after N cycles and E0 is the modulus in the uncycled state

## Slide 87: Monotonic Strength and Fracture Fatigue
We define the failure of the composite when a critical level of damage is reached or exceeded. Let D be the damage parameter that increases as a function of number of cycles, N. Then, dD/dN will be the damage growth rate. We can write for the damage growth rate:
where Δσ is the cyclic stress range, R is the stress ratio, and D is the current value of damage. Let Nf be the number of cycles to failure, i.e., the fatigue life corresponding to a critical level of damage. Then integrating previous equation between limits of initial damage, Di, and final damage, Df, we can write for the number of cycles to failure as

## Slide 88: Monotonic Strength and Fracture Fatigue
Modulus of the damaged material E is given by:
where c is a material constant.
For a given value of E/E0, we can write the modulus or stiffness reduction rate as:
where A and n are constants. The left hand side of this expression can be determined experimentally. Note that both sides are dimensionless quantities. The modulus reduction rate (−1/E0) dE/dN, at a given value of E/E0, is the tangent to the curve shown above.

## Slide 89: Monotonic Strength and Fracture Fatigue
Modulus reduction rate versus a parameter involving the peak stress
Number of cycles required to attain a given
stiffness reduction after cycling at different fractions of the ultimate tensile strength σUTS

## Slide 90: Monotonic Strength and Fracture Fatigue
Thermal stresses arise in composite materials due to the generally large differences in the thermal expansion coefficients (a) of the fiber and the matrix.
Thermal stresses in composites cannot be alleviated by slow cooling or some kind of annealing treatment, techniques that might work in conventional material. The reason for this is that the thermal mismatch will be there even if the temperature change is uniform throughout the volume of the composite.
Large internal stresses can result when fiber reinforced composites are heated or cooled through a temperature range. When this happens in a repeated manner, we have the phenomenon of thermal fatigue, because the cyclic stress is thermal in origin.
Thermal fatigue can cause cracking in the brittle polymeric matrix or plastic deformation in a ductile metallic matrix, cavitation in the matrix and fiber/ matrix debonding are other forms of damage.

## Slide 91: Monotonic Strength and Fracture Fatigue
Thermal cycle and the surface of SiCp/Al composite after thermal cycling. No damage is visible on the surface.
Same sample examined by X-ray tomography shows damage in the interior. Blue color shows cavitation, about 2% by volume. The SiC particles are about 25– 30 μm in diameter and 20% by vol.

## Slide 92: Monotonic Strength and Fracture Creep
Creep is defined as the time dependent deformation in a material.
It becomes important at relatively high temperatures, especially at temperatures greater than 0.4–0.5 TH, where TH is the homologous temperature equal to T/Tm, T is the temperature of interest in kelvin, and Tm is the melting point of the material in kelvin.
The phenomenon of creep can cause small deformations under a sustained load over a long period of time.
In a variety of situations or equipment (e.g., a pressure vessel or a rotating component), such slow deformations can lead to dimensional problems or even failure.
Pure dislocation creep, grain boundary sliding, vacancy motion in grains and in the grain boundaries, and dislocation can cause creep. The applied stress, grain size, porosity, and impurity content are important variables.

## Slide 93: Monotonic Strength and Fracture Creep
A creep curve, strain versus time, for a 25% Vf silicon carbide whisker/2124 aluminum alloy matrix
The steady-state creep rate as a function of applied stress for the unreinforced silver matrix and tungsten fiber/silver matrix composite at 600 °C

## Slide 94: Monotonic Strength and Fracture Creep
In very simple terms, creep in a PMC or MMC is likely to be dominated by the creep behavior of the matrix. As the matrix deforms in creep, the applied load is transferred to the load-bearing component, viz., fiber. Eventually, the fibers will carry all the load.
Introduction of creep resistant reinforcement, especially creep resistant fibers in a matrix that undergoes substantial creep, can result in a composite that is more creep resistant than the unreinforced matrix.
The minimum creep rate as a function of the applied stress for Saffil short fiber reinforced aluminum alloys and unreinforced aluminum alloys. Note that the creep rate for the composite is lower than that of the control alloy, but the stress exponent or slope of the composite is much higher than that of the unreinforced alloy